Photoconductive, dielectric and percolation properties of anodic TiO2 nanotubes studied by terahertz spectroscopy

Jiří Kuchařík1, Hanna Sopha2, Milos Krbal2, Ivan Rychetský1, Petr Kužel1, Jan M. Macak2, and Hynek Němec1,*

1Institute of Physics, Academy of Sciences of the Czech Republic, Na Slovance 2, 18221 Prague 8, Czech Republic

2Center of Materials and Nanotechnologies, Faculty of Chemical Technology, University of Pardubice, Nam. Cs. Legii 565, 53002 Pardubice, Czech Republic

* Corresponding author: e-mail nemec@fzu.cz

Abstract: Self-organized layers of anodic TiO2 nanotubes were investigated using time-resolved terahertz spectroscopy in the steady state and upon photoexcitation. The interpretation of the conductivity spectra is based on the response of confined charges calculated by the Monte-Carlo method and on the evaluated distribution of the probing terahertz electric field in the heterogeneous structure. We show that the charge motion perpendicular to the nanotube axis is confined on ~10 nm scale, and that the charge mobility inside these confinement areas is comparable to that observed in a bulk anatase crystal. The electrical connectivity between individual nanotubes assessed from the terahertz spectra qualitatively correlates with the geometry observed in SEM images. The measured transient terahertz transmission spectra feature an apparent resonance; we demonstrate that it is not a signature of a new low-energy excitation but a geometrical effect of Fabry-Pérot interferences in the photoexcited slab.

# 1. Introduction

Semiconductor titanium dioxide (TiO2) nanostructures represent promising materials in a variety of applications [1]. Self-organized vertically aligned TiO2 nanotube layers grown by anodization of titanium substrates have attracted a particular attention: these layers can be grown for a large range of nanotube diameters, wall thicknesses and lengths [2,3]. In the view of employing these highly ordered semiconductor nanostructures in photovoltaics and other photoelectrochemical applications, it is essential to understand their charge transport properties [4].

Measurements of dc conductivity provide a simple mean to describe charge transport from one electrode to the other, which is crucial information for applications. However, the complex nature of the TiO2 nanotube structure [2] makes it extremely difficult to decipher intrinsic properties of the nanotube walls from dc experiments – these properties are of fundamental interest as they determine the ultimate performance of nanotube devices. Interpretation of the standard conductivity measurements is further complicated by uncertainties in the electrode contact area on the top part of the nanotubes. This issue can be partly avoided by space-resolved probing using conductive atomic force microscopy (C-AFM) [5]. In any case, the long-range charge transport governing the dc conductivity in complex structures is restrained by the least efficient transport process. It is thus essential to identify this bottleneck process, in order to enable systematic optimization of the nanotube fabrication technology. For this purpose, one needs to obtain a detailed picture of the charge transport in the nanotube walls. A contactless probing by high-frequency terahertz (THz) radiation [6–8] disregards possible interactions of charges with distant defects and provides complementary and highly useful information about the charge transport on the nanometer scale [9]. In particular, a thoughtful analysis of terahertz spectra makes it possible to assess charge transport mechanisms, characteristic charge confinement distances, efficiency of the charge transport between nanoparticles and percolation degree of the (photo)conducting component [10–14]. All these pieces of information finally provide a comprehensive view of the charge transport and of its evolution shortly after photoexcitation.

In this paper we investigate both steady-state effective permittivity and photoinduced effective conductivity of layers of self-organized vertically aligned TiO2 nanotubes. Building up on previous reports on THz photoconductivity of TiO2 nanotubes prepared by anodization [15–17], we develop a microscopic model of their charge transport properties. The steady-state response (effective dielectric permittivity) reflects the distribution of the probing THz electric field in the TiO2 structure, i.e. it provides information about the morphology and interconnection of individual TiO2 nanotubes within the TiO2 layer [18, 19]. The photoinduced conductivity provides characteristics of the photoinitiated lateral charge transport in the nanotube walls.

Herein, we demonstrate that (i) photogenerated charges do not move freely inside the nanotube walls, but they are confined in regions with smaller (~10 nm) size, and that (ii) the degree of electrical connectivity between individual nanotubes determined from THz measurements qualitatively correlates with the geometrical connectivity inferred from SEM images. We also emphasize that quite sophisticated data analysis is required to reliably distinguish between real low-energy excitations in the conductivity spectrum and Fabry-Pérot interferences, which appear in the raw transient transmittance spectrum.

The paper is organized as follows. We first describe the preparation of the TiO2 self-organized nanotube layers by anodization, and briefly introduce the time-domain THz spectroscopy setup for measurements of the effective permittivity and photoconductivity (Section 2). In Sec. 3 we present the background theoretical models, including the effective medium approximation for the calculation of effective permittivity and effective photoconductivity, electromagnetic wave propagation in inhomogeneous photoexcited media for the determination of transient transmittance, and Monte-Carlo calculations of the THz conductivity. These are the key elements, which relate the morphology and intrinsic properties of TiO2 nanotube walls (encoded in effective permittivity and photoconductivity) with the measured transmittance and transient transmittance spectra. Finally, in Sec. 4, we compare our experimental spectra with the theoretical calculations and interpret the lateral charge transport in the TiO2 nanotube layers. Conclusions are drawn in Sec. 5.

# 2. Experimental section

## 2.1. Preparation of TiO2 nanotube layers by anodization

The electrochemical setup consisted of a 2 electrode configuration using a platinum foil as the counter electrode, while the Ti substrates (working electrodes) were pressed against an O-ring of the electrochemical cell, leaving 1 cm2 open to the electrolyte. Electrochemical experiments were carried out at room temperature employing a high-voltage potentiostat (PGU-200V, IPS Elektroniklabor GmbH).

Prior to anodization, the Ti substrates (Sigma-Aldrich, 0.127 mm, 99.7 % purity) were degreased by sonication in isopropanol and acetone, then rinsed with isopropanol and dried in air. The as-prepared Ti substrates were anodized using the above described setup at 60 V for 4 hours in an ethylene glycol based electrolyte containing 0.176 M NH4F and 1.5 vol.% H2O. All electrolytes were prepared from reagent grade chemicals and were aged for 15 h by anodization of a blank Ti foil before their use [20].

At the beginning of the anodization, the potential was swept to 60 V with a sweep rate of 1 V/s. After anodization, the Ti substrates were rinsed and sonicated in isopropanol and dried in air. Nanotube layers for THz spectroscopy were removed from underlying Ti substrates by dissolution of Ti in a Br2/methanol mixture, as published previously [17]. Morphological characterization of the TiO2 nanotube layers was carried out by using a field-emission scanning electron microscope (FE-SEM JEOL JSM 7500F). The inner diameters and the thicknesses of the TiO2 nanotube layers were evaluated by statistical analyses of the SEM images using proprietary Nanomeasure software. This careful and accurate approach is required for a reliable analysis of THz spectra of TiO2 nanotube layers, both in the ground and photoexcited state.

Examples of SEM images of the resulting nanotube layers are shown in figure 1(a-e). In line with previous reports [2,3], the nanotubes are open at the top, and closed at the bottom (where they were in contact with the Ti substrate before the removal). Closely packed individual nanotubes create a nanotube layer with thickness L of (30±2) μm and an average inner tube diameter of 120±10 nm.

Some of the samples were annealed at 400°C for 1 hour to achieve a crystalline structure without any change of nanotube dimensions. The crystallinity of annealed TiO2 nanotube layers was measured using the D8 Advance Bruker X-ray diffractometer set to Cu-Kα line. Measurement revealed polycrystalline anatase structure [figure 1(f)].

## 2.2. Terahertz spectroscopy

Measurements of complex THz transmittance in equilibrium and upon photoexcitation were performed in a standard experimental configuration [11] driven by an amplified femtosecond Ti:sapphire laser system (Spitfire Ace) delivering optical pulses at 800 nm with the repetition rate of 5 kHz. A part of the laser beam was used for the generation of THz pulses by optical rectification and their subsequent phase-sensitive detection by electro-optic sampling, both taking place in 1-mm thick (110) ZnTe crystals. The other part of the beam was frequency tripled and the resulting pulses at 266 nm (~4.66 eV) were used for the optical excitation of the studied nanotube layers. The pump photon energy is sufficient to ensure direct inter-band generation of conduction band carriers, since the bandgap of TiO2 in anatase phase is ~3.2 eV [21]. The pump beam was defocused to ensure homogeneous concentration of photocarriers across the probed region of the TiO2 nanotube layers (delimited by a 3 mm metallic aperture). The experiments were performed in a primary vacuum chamber to suppress the absorption of the THz beam by water vapor. The polarization of the THz beam was perpendicular to the nanotube axes, which allowed us to probe the in-plane (lateral) charge carrier transport.

# 3. Theoretical methods and data analysis

The goal of the theoretical analysis is to establish the relation between microscopic properties of the nanotubes (morphology of the nanotube layer, permittivity and photoconductivity of the nanotube walls), and the measurable THz signals, i.e. the steady-state transmittance spectrum T of the nanotube layer (without photoexcitation) and the relative photoinduced transmittance change T/T (=transient transmittance due to photoexcitation in pump-probe experiments). Three issues need to be considered as illustrated in figure 2:

1. Microscopic physical properties of TiO2 nanotube walls. The steady-state THz permittivity spectrum mic (without excitation) and optical absorption coefficient mic are considered to keep the values of the bulk anatase (mic ~ 30 with negligible dispersion [22], mic ~ 7×105 cm–1 at the excitation wavelength of 266 nm [23]). The mobility spectra  of photoexcited charges confined in the nanotube walls were calculated using Monte-Carlo method described in detail in Ref. [9]; the key underlying physics of this calculation is an extension of a Drude model, in which the charge carrier motion is confined into the nanotube wall). Apart from the nanotube wall geometry (=shape, nanotube diameter and the thickness of nanotube wall), the inputs are the effective charge (polaron) mass m* and its mean scattering time s inside the nanotube walls (this is the intrinsic relaxation time involving isotropic scattering events in the volume of nanotube walls but not involving the interaction of charges with the nanotube surfaces). There is an ongoing debate on effective masses of electron and hole polarons in anatase [24]; values in the range from ~0.4 to ~10 (in free electron mass units) have been reported for electrons and holes [25–27] and it is still unclear whether electrons are lighter than holes or vice versa; the discussion is further complicated by the anisotropy of the effective masses. In our work we cannot distinguish the polarity of carriers participating to the THz photoconductivity; however, it seems to follow from both experimental and theoretical works that the lighter polaron’s effective mass is near 1 or 2 [24,27,28]. Since the conductivity is usually dominated by carriers with the lower effective mass, we considered the effective mass of the carriers to be equal to 1 in our Monte-Carlo calculations.

As we will argue later, the motion of charges restricted solely by the physical nanotube boundaries is not compatible with the observed transient conductivity spectrum and clearly an assumption of a stronger confinement is required. For this reason, we developed calculations in which we introduced an additional interaction. To emulate the additional confinement, we considered an internal structure inside the nanotubes consisting of confining nanoregions modeled by a set of cubes with the dimension a [figure 2(a)]. When a carrier hits the boundary of a nanoregion during its motion, it is scattered; with the probability pF the carrier enters the adjacent cube upon this scattering event and with the probability 1 – pF it remains in the original cube (preferential backscattering). The confinement size a, the mean scattering time τs, and the probability pF are the adjustable parameters of these calculations. Note that pF = 0.5 describes the case of isotropic scattering, i.e., pF has to be close to 0 (much smaller than 0.5) to produce a significant confining effect of the nanoregions.

The transient microscopic conductivity mic in the nanotube walls is related to the mobility μ of photoexcited charges:

Δσmic(ω)=eNμ(ω) ,	(1)

where N is the photocarrier concentration and e is the elementary charge. Both μ and mic describe the response to the local THz electric field inside the nanotube walls. Since the nanotube layer is a composite of TiO2 nanotube walls interleaved with vacuum, the probing field is not distributed homogeneously and therefore the THz field inside the nanotube walls differs from the intensity of the THz pulse. This phenomenon is accounted for in the next step by evaluating effective properties of the entire nanotube layer.

2. Effective medium approximation is the key approach which takes into account the influence of the morphology of the structure. It transforms the microscopic properties of components [i.e., properties of the photoconducting nanotube walls (mic, mic and mic) as well as the properties of the vacuum surrounding the nanotube walls] into the effective properties of the entire nanotube layer: effective THz permittivity without photoexcitation eff, effective absorption coefficient of the excitation beam eff, and effective transient conductivity spectrum eff(ω). The homogenization procedure enables convenient description of the propagation of both probing THz wave and UV excitation beams throughout the nanotube layer.

Since the effective properties of a nanotube layer are strongly sensitive to the percolation state of the nanotubes, we first examined several model morphologies with various percolation degrees such as those shown in Tab. 1. Numerical calculations of the quasi-static electric field spatial distribution inside these structures were performed using finite element method. The field distribution was then used to determine the effective properties of the structures, as described in detail in [18]; the effective optical absorption eff was calculated using the same quasi-static approach similarly as in [13]. It should be stressed that the same morphology has been used to calculate the effective properties both in the THz (eff and eff) and in the optical (eff) spectral ranges.

As pointed out earlier, anatase exhibits only a weak dispersion of mic in the spectral region of interest; a single value then can also characterize the effective steady state permittivity eff. Similarly, a single value of eff represents the effective exponential decay of the pump beam (Lambert-Beer absorption law) in the sample structure at the excitation wavelength of 266 nm (Tab. 1). In contrast, the transient effective conductivity eff is expected to exhibit a significant spectral dependence. It can be related to the transient conductivity of the nanotube walls as follows [18]:

Δσeff =VΔσmic+BΔσmic1+iDΔσmic/ωε0 ,	(2)

where ω = 2f is angular frequency and 0 is the permittivity of vacuum. Eq. (2) stems from the Bergman spectral representation of effective medium as discussed in detail in [18] and [29] and it is a convenient mean which very accurately encapsulates results of time-consuming numerical calculations into a simple formula enabling understanding the role of depolarization fields within an analytical framework. The morphology coefficients V and B can be approximately identified with the weights of the percolated pathways and non-percolated pathways, respectively, while the morphological coefficient D is related to the dominant depolarization factor. The coefficient V vanishes in non-percolated structures, while in percolated structures it is non-zero and in this case the V-term usually dominates over the B-term.

The diameter of the nanotubes is only about a half of the excitation wavelength. Under such conditions, interference may lead to a laterally slightly inhomogeneous excitation of the nanotube walls immediately after photoexcitation. The related slight variation of the microscopic conductivity cannot significantly influence the effective photoconductivity (the key parameter here is the abrupt step between the photoconducting nanotube wall and its isolating surroundings); moreover, the excitation density is further smoothed within the probing time (10 ps after photoexcitation) due to the charge carrier diffusion.

3. THz wave propagation in the nanotube layer. The complex transmittance of an unexcited self-standing optically thin layer (all internal Fabry-Pérot reflections are summed up as they cannot be resolved in time) with thickness L and complex THz (effective) refractive index n reads [30]

T=4nn+12∙exp⁡[ikn-1L]1-n-1n+12exp2iknL ,	(3)

where k = ω/c is the wave vector of the freely propagating THz radiation and c is the speed of light in vacuum. Numerical solution of this equation yields the effective permittivity of the unexcited studied sample, eff = n2 [30].

In optical pump – THz probe experiments, a transient THz transmittance spectrum ΔEt/Et is measured, where Et is the spectrum of the THz pulse transmitted through the sample in equilibrium, and ΔEt is its photo-induced change. We represent the measured data in the form of normalized transient transmission ΔTnorm [29], defined for a free-standing layer as

∆Tnorm=-2z0e0ϕΔEtωEtω ,	(4)

where ϕ is the optical pump photon fluence (expressed in number of photons per pulse and per unit area), z0 is the vacuum wave impedance, and e0 is the elementary charge. For monolithic materials, ΔTnorm directly represents the product of the quantum yield of photocarrier generation and of the mobility of photocarriers [29,31]. In heterogeneous systems, the dependence of ΔTnorm on the photocarrier mobility can be fundamentally more complicated due to the presence of depolarization fields and due to the depth gradient of the photocarrier density related to the absorption of the excitation beam following the Lambert-Beer law. Indeed, due to the strong absorption at 266 nm, charges are generated only in the top part of the nanotubes layer, as illustrated in figure 2 while we can safely neglect the excitation density in the bottom part [i.e., exp-αeffL≈0]. Here we base the analysis entirely on our theory developed and discussed in [29], namely on a general equation (42) or Eqs. (22) for the percolated case and (36) for the non-percolated case. These formulas take into account the Fabry-Pérot reflections, heterogeneous nature of the investigated structure and the depth gradient of the photocarrier density. They provide a recipe how to evaluate ΔTnorm in various experimental cases (see figure 4 in [29] and the relevant discussion therein). In the general case ΔTnorm may depend on the photocarrier concentration (pump fluence); later in this paper the experimental spectra will reveal that ΔTnorm does not depend on the pump fluence and this fact is very important for the elucidation of the sample morphology. In order to simplify the mathematical description and the discussion from the very beginning we now identify the situations, for which ΔTnorm is fluence independent, and formulas, which describe this case.

It follows from [29] that ΔTnorm does not depend on the carrier concentration in the range of available pump fluences if any of the following conditions is fulfilled:

1. The sample is essentially percolated, i.e. V ≫ B.

2. The sample is non-percolated (or weakly percolated) but the D-term in Eq. (2) is small: Dmic/(ωε0) ≪ 1. This can happen for morphologies close to the percolation (very small D) or for small mic (which implies low carrier density or low mobility).

The most general formula describing these cases under the specified conditions can be easily derived from Eq. (22) in [29]; it reads:

∆Tnorm= 1nAV+Bαmicαeffξμ1+r1r2exp2ikL+r11-2ik/αeff+ r2exp2ikL1+2ik/αeff.	(5)

Here ξ is the quantum yield of photogenerated carriers, r1 = r2 = (n – 1)/(n + 1) are the reflection coefficients on the inner sample surfaces, and the term A= 1-r1r2exp2ikL-1 describes the Fabry-Pérot reflections of the transient wave inside the TiO2 nanotube layer. This formula will be used for the analysis of experimental spectra.

# 4. Results and Discussion

## 4.1. Effective Permittivity

The effective permittivity in the steady state is controlled by the permittivity of the constituents and by their shape and filling factors. Its value significantly increases above the percolation threshold of the TiO2 component: this is illustrated in Tab. 1 for representative model structures with similar filling factors, but different percolation degrees.

The measured steady-state effective permittivity of both amorphous and anatase TiO2 nanotube layers is about 8 – 9 (figure 3), i.e., it is close to the calculated permittivity of the model structure P1 and considerably higher than the permittivity calculated for the non-percolated model structures N1 and N2 (Tab. 1). We thus conclude that the nanotubes within the layers are to some extent electrically interconnected. This is further supported by the fact that the nanotube layers hold together; they do not disintegrate spontaneously upon manipulation. At the same time, it follows from these steady-state measurements that the contact area cannot be very large in comparison with the total outer surface of nanotubes: for example, the structure P2 containing overlapping tubular regions exhibits an effective permittivity significantly higher than the measured one. The essential property enabling a good match of the model to the measured effective permittivity is thus a weak average connectivity.

Now we have to elaborate on a comparison with the SEM results (figure 1). Although these images evoke closely packed arrangements, a detailed inspection of the top part [figure 1(a)] shows that narrow gaps do exist between many of the nanotubes. A similar conclusion about the presence of both connected and disconnected nanotubes can be drawn also from the cross-sectional views [figure 1(b–e)]. To avoid difficult calculations accounting for the presence of both isolated and interconnected nanotubes, we represented their structure by the simplified model structure P1 characterized by a weak average connectivity. In this sense, the morphology of the nanotubes inferred from effective permittivity correlates with the SEM images.

We are aware that a single value of the effective permittivity cannot completely elucidate the real morphology; it provides solely an estimate of the average connectivity. This knowledge is nevertheless essential for the subsequent analysis of the transient photoconductivity, since it allows a reliable estimation of the effective-medium parameters V and B and of the optical properties such as the ratio mic/eff (Tab. 1) entering Eq. (5). Note that in the case of P1 we obtain B ≪ V; we will thus neglect the B-terms in further analysis.

## 4.2. Transient Photoconductivity

Examples of normalized transient transmission spectra are shown in figure 4(a). Only crystalline TiO2 nanotubes photoexcited from the side of their open tops show a significant response. Their transient conductivity is long lived; the initial decay rate is on the hundreds-picosecond time scale and it seems to slow down further after ~500 ps [figure 4(c)]. Amorphous TiO2 nanotubes do not exhibit any measurable signal even at the shortest pump-probe delays (~1 ps), implying that |ΔTnorm| ≲ 0.02 cm2V–1s–1. The response of crystalline TiO2 nanotubes excited from the bottom part ΔTnorm ~ 0.05 cm2V–1s–1 is close to the detection limit of our setup. The bottom part corresponds to the area where electric-field-aided anodic oxidation of the Ti foil takes place, therefore it is not surprising that its properties differ from those of the rest of the nanotube walls where the oxidation process is already completed.

In the next discussion, we will focus on the anatase nanotube layers excited from the top. There is no significant dependence of ΔTnorm on the excitation fluence [figure 4(a)]. This result clearly supports the finding that the nanotube layers are percolated. We verified by a calculation that the general equation (42) from Ref. [29]—valid for both percolated and non-percolated structures—would necessarily lead to fluence-dependent spectra for the structures N1 and N2 for the pump fluences used in the experiments, while no fluence dependence would be obtained for percolated systems P1 and P2. This also justifies the use of Eq. (5) for retrieving the mobility spectra of our samples.

The spectrum of ΔTnorm exhibits a resonant-like behavior. Although a similar feature has been observed in Ref. [15] and attributed to the response of excitons, we can prove that in our spectra it is an interference maximum in the TiO2 nanotube layer with thickness of 30±2 μm. Indeed, the spectrum of the mobility retrieved from the ΔTnorm using Eq. (5)—which correctly accounts for the interferences—is smooth [figure 4(b)], with no signature of a sharp resonant behavior, and its shape features typical signatures of the charge confinement: increasing real part and negative imaginary part. Similar complicated interference patterns have been observed also in the ΔTnorm of ~200 m thick nanocrystalline Si samples [32]: the same model as we use here was able to deconvolute them successfully and reveal a featureless effective response function. It should be noted that the errors in the mobility spectra retrieved from ΔTnorm (involving the noise in ΔTnorm spectra as well as uncertainties in the sample thickness) are amplified in the vicinity of the interference maxima. This is the main reason why the reliable mobility spectra are obtained in a narrower frequency range than the ΔTnorm spectra [figure 4(a,b)].

Monte-Carlo calculations of the charge mobility in TiO2 nanotube walls without any additional interaction provide spectra with a shape incompatible with the observed ones (a = ∞ in figure 5): the increase of the calculated real part with frequency is much slower, and also the calculated imaginary part has a minimum at lower frequency than observed in experiments. Since the peak frequency is inversely proportional to the confinement length [9], we infer that the charges must be confined more strongly than just by the nanotube walls.

In figure 6, we illustrate the response of a few model structures in order to devise the mechanism responsible for the observed spectral shape. Confinement effects in 140-nm diameter nanocylinders are marginal since the carrier mean free path is much smaller than the nanocylinder diameter. In the nanotubes, the carriers are confined only partially: although the confinement by the 10-nm thick walls is important, charges can still move freely along the circumference of the nanotube walls. More severe confinement is achieved only when the motion in all directions is blocked: this can be achieved e.g. when the nanotube walls are divided into smaller regions separated by high potential barriers (preventing linear charge transport among these areas) as schematically shown in figure 2(a).

A particularly good match with experimental data is when the nanotube walls are divided into regions with characteristic size a = 10 nm, see figure 5. The probability of the charge carrier transport among adjacent nanoregions is pF ≈ 2.5%. This suggests that the nanotube walls may be composed of such small anatase nanograins. Furthermore, another confining mechanism may exist: band bending of TiO2 [33,34] may confine charges of one polarity close to the nanotube wall surfaces and the other close to the central part of the annulus of nanotube walls, thus making their motion more sensitive to a possible presence of surface defects. It is interesting to notice in figure 5 that the correct increase of the real part of the conductivity can be achieved only for calculations with longer scattering times (s = 15 fs). This corresponds to a rather high Drude mobility (e0s/m* ~ 30 cm2V–1s–1 – note that this is only an order of magnitude estimate namely due to the ambiguity in the effective mass m* entering the Monte-Carlo calculations, and, to some extent, also due to the uncertainty of the adjustable parameters a and s), comparable with the one obtained in high-quality intrinsic or niobium doped crystalline anatase at room temperature [35,36]. Indeed, this is the ultimate mobility value which would be achieved if one were able to get rid of the confining nanoregions inside the nanotubes. The small amplitude of the measured signal (compared to the high Drude mobility) implies a low yield ( = 10% as determined by amplitude fitting), which we attribute to the presence of a high density of deep traps at the nanotube wall surfaces. Since the used short-wavelength excitation (the penetration depth for this wavelength in anatase is ~ 15 nm) generates a significant fraction of charges close to these traps, the overall quantum yield of mobile charges may be reduced. Similar conclusion was drawn also for electrons in InP nanowires [37].

These findings are quite striking in the view of THz conductivity spectra of other crystalline TiO2 nanotube layers prepared by anodization of Ti: an excitonic response superposed on a power-law conductivity was observed by Richter et al. [15], a Drude-like mobility spectra with very small amplitude were reported by Wehrenfennig et al. [16], and an extremely small conductivity with the spectra characteristic for weakly localized charge carriers was observed by us on much lower aspect ratio nanotube layers [17]. These results clearly suggest that the charge transport properties of TiO2 nanotube layers sensibly depend on the protocol of the nanotube preparation.

# 5. Conclusions

Time-domain terahertz spectroscopy was employed to characterize self-organized anodic TiO2 nanotube layers. A careful analysis made it possible to reliably determine their effective THz permittivity and effective THz photoconductivity. In particular, we demonstrated that the observed apparent resonance in transient terahertz transmission spectra is caused by Fabry-Pérot interferences in the film, and not by an additional low-energy excitation.

The measurement and analysis of the effective steady-state permittivity provided a mean to assess the in-plane electrical connectivity of the nanotubes. We showed that the electrical connectivity qualitatively correlates with the geometrical nanotube connectivity observed in SEM images. The terahertz photoconductivity spectra exhibit a pronounced dispersion which suggests—in the light of Monte-Carlo calculations of the THz conductivity—a confinement of charges on distances ~10 nm, thus indicating that there are obstacles for the charge motion along the circumference of the nanotube walls. The mobility of charges inside the confinement areas is comparable to that of the bulk TiO2 anatase: there is thus a room for further optimization of anodization protocol to result into TiO2 nanotube layers with suppressed confining barriers, which would lead to a material with excellent long-distance charge mobility.

# 6. References

[1]	Special Issue on Titanium Dioxide Nanomaterials. Chem. Rev. 114 (2014).

[2]	J. M. Macak, H. Tsuchiya, A. Ghicov, K. Yasuda, R. Hahn, S. Bauer, and P. Schmuki, Curr. Opin. Solid State Mater. Sci. 11, 3 (2007).

[3]	K. Lee, A. Mazare, and P. Schmuki, Chem. Rev. 114, 9385 (2014).

[4]	J. A. Anta, Curr. Opin. Solid State Mater. Sci. 17, 124–131 (2012).

[5]	S. Das, R. Zazpe, J. Prikryl, P. Knotek, M. Krbal, H. Sopha, V. Podzemna, and Jan M. Macak, Electrochim. Acta 213, 452 (2016).

[6]	C. A. Schmuttenmaer, Chem. Rev. 104, 1759 (2004).

[7]	Grüner, G. Millimeter and Submillimeter Wave Spectroscopy of Solids; 1998, Springer-Verlag, Berlin, Heidelberg.

[8]	R. Ulbricht, E. Hendry, J. Shan, T. F. Heinz, and M. Bonn, Rev. Mod. Phys. 83, 543 (2011).

[9]	H. Němec, P. Kužel, and V. Sundström, Phys. Rev. B 79, 115309 (2009).

[10]	F. A. Hegmann, O. Ostroverkhova, and D. G. Cooke, Probing organic semiconductors with terahertz pulses. In: Photophysics of Molecular Materials, pp. 367–428, Wiley-VCH Verlag GmbH &Co. KGaA, Weinheim (2006).

[11]	L. Fekete, P. Kužel, H. Němec, F. Kadlec, A. Dejneka, J. Stuchlík, and A. Fejfar, Phys. Rev. B 79, 115306 (2009).

[12]	V. Skoromets, H. Němec, J. Kopeček, P. Kužel, K. Peters, D. Fattakhova-Rohlfing, A. Vetushka, M. Müller, K. Ganzerová, and A. Fejfar, J. Phys. Chem. C 119, 19485 (2015).

[13]	H. Němec, V. Zajac, P. Kužel, P. Malý, S. Gutsch, D. Hiller, and M. Zacharias, Phys. Rev. B 91, 195443 (2015).

[14]	Z. Mics, H. Němec, I. Rychetský, P. Kužel, P. Formánek, P. Malý, and P. Němec, Phys. Rev. B 83, 155326 (2011).

[15]	C. Richter and C. A. Schmuttenmaer, Nat. Nanotechnol. 5, 769 (2010).

[16]	C. Wehrenfennig, C. M. Palumbiny, H. J. Snaith, M. B. Johnston, L. Schmidt-Mende, and L. M. Herz, J. Phys. Chem. C 119, 9159 (2015).

[17]	M. Krbal, J. Kuchařík, H. Sopha, H. Němec, and J. M. Macák, Phys. Status Solidi Rapid Res. Lett. 10, 691 (2016).

[18]	H. Němec, V. Zajac, I. Rychetský, D. Fattakhova-Rohlfing, B. Mandlmeier, Z. Mics, and P. Kužel. IEEE Trans. Terahertz Sci. Technol. 3, 302 (2013).

[19]	S. A. Jensen, K.-J. Tielrooij, E. Hendry, M. Bonn, I. Rychetský, and H. Němec, J. Phys. Chem. C 118, 1191 (2014).

[20]	H. Sopha, L. Hromadko, K. Nechvilova, and J. M. Macak, J. Electroanal. Chem. 759, 122 (2015).

[21]	H. Tang, H. Berger, P. E. Schmid, F. Lévy, and G. Burri, Solid State Commun. 87, 847 (1993).

[22]	R. J. Gonzalez, R. Zallen, and H. Berger, Phys. Rev. B 55, 7014 (1997).

[23]	G. E. Jellison Jr., L. A. Boatner, J. D. Budai, B.-S. Jeong, and D. P. Norton, J. Appl. Phys. 93, 9537 (2003).

[24]	T. Luttrell, S. Halpegamage, J. Tao, A. Kramer, E. Sutter, and M. Batzill, Sci. Rep. 4, 4043 (2014).

[25]	Y. Furubayashi, N. Yamada, Y. Hirose, Y. Yamamoto, M. Otani, T. Hitosugi, T. Shimada, and T. Hasegawa, J. Appl. Phys. 101, 093705 (2007).

[26]	M. Dou, and C. Persson, J. Appl. Phys. 113, 083703 (2013).

[27]	B. Enright and D. Fitzmaurice, J. Phys. Chem. 100, 1027 (1996).

[28]	C. Kormann, D. W. Bahnemann, and M. R. Hoffmann, J. Phys. Chem. 92, 5196 (1988).

[29]	P. Kužel and H. Němec, J. Phys. D: Appl. Phys. 47, 374005 (2014).

[30]	L. Duvillaret, F. Garet, and J.-L. Coutaz, IEEE J. Selected Topics in Quantum Electron. 2, 739 (1996).

[31]	P. Tiwana, P. Parkinson, M. B. Johnston, H. J. Snaith, and L. M. Herz, J. Phys. Chem. C 114, 1365 (2010).

[32]	V. Zajac, H. Němec, C. Kadlec, K. Kůsová, I. Pelant, and P. Kužel, New J. Phys. 16, 093013 (2014).

[33]	J. Lloyd-Hughes, S. K. E. Merchant, L. Sirbu, I. M. Tiginyanu, and M. B. Johnston, Phys. Rev. B 78, 085320 (2008).

[34]	M. Anpo, K. Chiba, M. Tomonari, S. Coluccia, M. Che, and M. A. Fox, Bull. Chem. Soc. Jpn. 64, 543 (1991).

[35]	L. Forro, O. Chauvet, D. Emin, L. Zuppiroli, H. Berger, and F. Lévy, J. Appl. Phys. 75, 633 (1994).

[36]	Y. Furubayashi, T. Hitosugi, Y. Yamamoto, K. Inaba, G. Kinoda, Y. Hirose, T. Shimada, and T. A. Hasegawa, Appl. Phys. Lett. 86, 252101 (2005).

[37]	C. S. Ponseca, Jr., H. Němec, J. Wallentin, N. Anttu, J. P. Beech, A. Iqbal, M. Borgström, M.-E. Pistol, L. Samuelson, and A. Yartsev, Phys. Rev. B 90, 085405 (2014).

# Acknowledgments

European Research Council and Ministry of Youth, Education and Sports of the Czech Republic and Czech Science Foundation are acknowledged for financial support of this work through projects 638857, LM2015082, and 17-03662S, respectively. J.M. and H.N. are grateful to the Neuron Fund for Support of Science for initiating our collaboration. We thank Dr. Veronika Podzemna and Ludek Hromadko for SEM analyses, Assoc. Prof. Ludvik Benes for XRD analyses.

|  | structure | εeff | αmic/αeff | V | B | D | s |
| --- | --- | --- | --- | --- | --- | --- | --- |
| N1 |  | 4.4 | 7.7 | 0 | 0.05 | 0.019 | 39% |
| N2 |  | 5.6 | 6.1 | 0 | 0.09 | 0.015 | 43% |
| P1 |  | 8.4 | 4.8 | 0.24 | 0.0028 | 0.027 | 44% |
| P2 |  | 10.4 | 4.0 | 0.32 | 0.0005 | 0.032 | 49% |

Tab. 1. Summary of effective properties of selected model geometries of nanotubes (black areas = TiO2, white areas = air/vacuum; N1, N2 – isolated nanotubes with different gaps between them; P1, P2 – percolated nanotubes with different connectivity). Parameters of calculations: THz permittivity of anatase without photoexcitation = 30 [13]; refractive index of anatase at 266 nm = 3 [14], absorption coefficient of anatase at 266 nm = 7×105 cm–1 [14]. Morphology coefficients V, B, and D are defined by Eq. (1). The parameter s is the volume filling fraction of TiO2 in the nanotube layer.

Figure 1. SEM images of self-organized TiO2 nanotube layer: (a) top-view and (b–e) cross-section. Images (c–e) are taken at high magnification. (f) X-ray diffraction pattern of the annealed TiO2 nanotube layer. The titanium peaks come from the Ti substrate underneath the nanotube layer.

120 nm

120 nm

Figure 2. Illustrations of the steps in theoretical calculations of the THz spectra. The indicated outputs identify the quantities calculated in each step of the model while the rest indicates the most important input parameters for the given step. (a) Monte-Carlo calculations are employed to calculate evolution of thermal charge trajectories (red curve) in an isolated nanotube; the Kubo formula then provides the microscopic transient conductivity spectrum mic. The dashed lines denote planes where we assume a possible backscattering of charges with the probability 1 – pF. (b) Effective medium approximation is applied to transform the microscopic permittivity mic and transient conductivity mic of the nanotube walls into the effective conductivity of the nanotube layer. (c) Finally, the steady-state and transient transmission functions T and Tnorm are calculated, respectively. With the pump beam on, the excitation density decreases with depth and the wave equation is solved under such conditions [21] in order to take into account properly the interferences of the THz beam in the photoexcited nanotube layers.

Figure 3. Measured spectra of the permittivity of anatase and amorphous nanotube layers (without photoexcitation). Closed symbols: real part; open symbols: imaginary part. The dotted horizontal lines indicate real parts of the permittivities calculated for the model structures shown in Tab. 1.

Figure 4. (a) Spectra of the normalized transient transmission of anatase and amorphous TiO2 nanotube layers excited from the top and from the bottom of the layers, measured 10 ps after photoexcitation. Closed symbols: real part, open symbols: imaginary part. (b) Spectra of the product V×ξμ(ω) calculated from Eq. (5) for nanotube layers excited from the top. The lines in both panels serve as guides for the eye only. (c) Decay of an average THz photoconductivity with time in nanotube layers excited from the top.

Figure 5. Spectra of the charge mobility in the model structure from figure 2(a) obtained by Monte-Carlo calculations for various sizes of the cubic regions a (lines); example of the experimental spectrum with  = 5.7 × 1013 photons/cm2 (symbols). The values of the quantum yield , scattering time s and the probability pF of the transport among the confinement nanoregions were optimized to find the best match of the calculated spectra to the measured data; values of  and s are summarized in the plot, pF = 2.5% for all the spectra shown. The curve with a = ∞ corresponds to homogeneous nanotube walls, without the confinement regions.

Figure 6. Examples of charge mobility spectra calculated by Monte-Carlo method for various confinement environments [outer diameter = 140 nm for all nanostructures, nanotube wall thickness = 10 nm; “Nanoregion” identifies nanotube wall divided into 10-nm cubic regions as sketched in figure 2(a)]. At high frequencies the mobility of carriers is determined by their inertia and therefore it follows the same behavior for all the structures. In the bulk the dc mobility (real part) is non-zero since there are no obstacles for the carrier motion, whereas it vanishes in all nanostructures as they are isolated from the surroundings. Confinement of charges thus leads to a drop of the real part of the mobility at low frequencies; the cross-over frequency essentially depends on the characteristic confinement distance. The imaginary part of the mobility is conform to the Kramers-Kronig transformation of the real part.