CrystEngComm, 2016 016, 18, 2843–2851

Crystal morphology of 3,4-bisĲ3-nitrofurazan-4-yl)furoxan (DNTF) in a solvent system: molecular dynamics simulation and sensitivity study

Ning Liu, Ya-nan Li, Svatopluk Zeman, Yuan-jie Shu, Bo-zhou Wang,Yan-shui Zhou, Qiang-li Zhao  and Wen-liang Wang

Backround:

High energy density materials (HEDM) have gained increasing attention in recent years because of their applications for military purposes as propellants, explosives, and pyrotechnics and civilian use in mining and demolition. However, it is unfortunate that many energetic materials with high energy content are concomitantly sensitive, which enhances the risk of accident during synthesis and handling. For energetic materials, crystal morphology research constitutes an important aspect since sensitivity is greatly affected by the shape, size and arrangement of the crystal, which means a low sensitivity can be achieved only by changing the shape and size of crystals with the same components.

3,4-bis(3-nitrofurazan-4-yl)furoxan (DNTF) is an example of a new HEDM in which problem is that the crude products cannot be used directly because of the irregular morphology and low purity. Therefore, recrystallization is a key step in the application of DNTF by controlling the crystal morphology, size and purity.

Material and Methods:

The starting DNTF material was prepared according to the literature. Recrystallization was realized in a round-bottomed flask was charged with 10 g DNTF and 60 mL solvent (AcOH :H2O = 65 : 35 or EtOH :H2O = 75 : 25 in mass ratio). The solution was heated from room temperature to 70 °C by stirring at a certain speed in an oil bath to make it dissolve completely. The impact sensitivity test was determined according to the Chinese GJB-772A-97 standard method 601.2 with a WL-1type impact sensitivity instrument.

The attachment energy (AE) model is widely used to predict crystal morphologies of explosives and pharmaceuticals; it was proposed by Hartman based on the period bond chain (PBC) theory. For the energies of the system, taking the crystal unit cell into account, the AE model can predict the morphology more precisely than the BFDH method. By the AE method, the morphologies of certain crystals can be deduced by the center to- plane distance assigned to the dominant crystal surface,

which relates to the relative growth rate. In the present paper all the simulations were implemented using the program Materials Studio 5.5 (Accelrys Inc., USA). The COMPASS force field was chosen to predict the structures and properties of DNTF crystals.

Results:

The crystal morphology of DNTF in a vacuum was calculated by the AE model. It may be concluded that the adsorption of solvent molecules is facilitative on the abovementioned faces. For (1 1 0) and (1 1 1) faces, the relatively low S values mean morphological smoothness, which makes the adsorption behaviors less favorable. In addition, the polar nitro groups are found to be exposed at all five surfaces, and only the (0 1 1) face shows the exposure of polar oxygen atoms. This suggests that all faces could be classified as polar surfaces because of the exposed nitro groups, which is conducive to the adsorption of polar solvents. In order to study the affinity of solvent molecules for different DNTF crystal faces, the adsorption behaviors of the solvents were thoroughly investigated. From the previous theory, the vacuum attachment energies of DNTF crystal faces would be altered by the interactions of the solvent layer. The large value of the diffusion coefficient indicates the strong interaction between solvent molecules and surfaces; therefore, the relative growth rates of (0 0 1) and (0 1 1) faces become slower and the morphological importance increases. On the contrary, the D values of solvent on the (1 1 1) face in H2O/AcOH solvent and the (1 1 0) face in H2O/EtOH solvent are the lowest in the respective systems; the growth rate will improve accordingly and the corresponding faces will probably disappear. This is in reasonably good agreement with experimental results. Sensitivity measurements prove that the sensitivity of explosives could be altered effectively by means of modifying the crystal morphology, and the mixture of H2O/AcOH could be the recommended solvent in the practical application of purification of DNTF.

Conclusion:

In summary, by using molecular dynamics simulations of theinterface adsorption models between the DNTF crystal surface and the solvent layer, the crystal morphologies of DNTF in the solvents H2O/AcOH and H2O/EtOH were investigated based on the corrected AE model. The morphologically dominant faces of DNTF in a vacuum are (0 1 1), (0 0 1), (1 0 1), (11 0) and (1 1 1), predicted using the AE model. The crystal packing diagrams of DNTF habit faces indicate that all five faces could be classified as polar surfaces, whereas the (0 1 1) and (0 0 1) faces have relatively rough surface topographies. By calculating the corrected attachment energy, the (0 1 1) and (0 0 1) faces were found to be the morphologically important growth faces in both H2O/AcOH and H2O/EtOH solvent systems. The crystal shapes of DNTF in the H2O/AcOH and H2O/EtOH solvents are plate-shaped and rod-shaped, respectively, which is in agreement with the experimental results. Moreover, the RDF analysis shows that the adsorption behaviors of the H2O molecules on DNTF surfaces comprise hydrogen bonds, vdW forces and Coulomb interactions, whereas only vdW and Coulomb interactions exist betweent AcOH (EtOH) molecules and DNTF surfaces. Because of the high values of the diffusion coefficients, the growth rates of (0 0 1) and (0 1 1) faces are inhibited, making them the dominant growth faces. Finally, sensitivity tests indicate that the crystals cultivated from the H2O/AcOH solvent display improved stability to friction sensitivity in comparison with those of H2O/EtOH. This study offers a foundation for exploring more attractive strategies for reducing the sensitivity of the highly

sensitive explosives.