This is the accepted version of the following article:

## Janicek, P., Funke, S., Thiesen, P.H., Slang, S., Palka, K., Mistrik, J., Grinco, M., & Vlcek, M. (2018).  Electron beam induced changes in optical properties of glassy As35S65 chalcogenide thin films studied by imaging ellipsometry. Thin Solids Films, 660, pp. 759-765. doi: 10.1016/j.tsf.2018.03.079

This postprint version is available from URI  https://hdl.handle.net/10195/72631

Publisher’s version is available from

https://www.sciencedirect.com/science/article/pii/S0040609018302293?via%3Dihub

This postprint version is licenced under a Creative Commons Attribution-NonCommercial-NoDerivatives 4.0.International.

Electron beam induced changes in optical properties of glassy As35S65 chalcogenide thin films studied by imaging ellipsometry

P. Janicek1,2,*, S. Funke3, P. H. Thiesen3, S. Slang2, K. Palka4,2, J. Mistrik1,2, M. Grinco2, M. Vlcek2

1 Institute of Applied Physics and Mathematics, Faculty of Chemical Technology, University of Pardubice, Studentska 95, Pardubice 532 10, Czech Republic

2 Center of Materials and Nanotechnologies, Faculty of Chemical Technology, University of Pardubice, Studentska 95, Pardubice 532 10, Czech Republic

3 Accurion GmbH, Stresemannstrasse 30, 37073 Göttingen

4 Department of General and Inorganic Chemistry, Faculty of Chemical Technology, University of Pardubice, Studentska 95, Pardubice 532 10, Czech Republic

* The corresponding author e-mail: petr.janicek@upce.cz

Keywords: imaging ellipsometry, optical properties, chalcogenide glass, thin films, micro-structuring

Abstract

Spectroscopic imaging ellipsometry was used to study 50 µm  50 µm squares recorded into glassy As35S65 thin film by electron beam with different exposure doses. Optical constants (refractive index n and extinction coefficient k) of electron exposed areas were determined from imaging ellipsometric data recorded over a spectral range 390 – 800 nm. Complex dielectric permittivity of each of electron exposed square (glassy As35S65 with different electron exposure dose) was parametrized by a Tauc-Lorentz oscillator. Gradient optical model with the refractive index changing linearly within the layer thickness was used.

Evaluation of parameters of Tauc-Lorentz oscillator revealed decrease of energy bandgap, increase of the refractive index in whole recorded spectra (more pronounced at the top of the film) and increase of extinction coefficient in the part of spectra where the material absorbs with the increasing electron exposure dose used for exposure of the squares.

The decrease in local disorder with increasing electron exposure dose is quantified from the short wavelength absorption edge onset using a Mott-Davis model. The dependence of the parameters of Wemple-DiDomenico model for the transparent part of the optical constants spectra on electron exposure dose is shown.

Thin film with recorded image was subsequently etched in amine based solution in aprotic solvent. While native film was fully etched off the remaining height of the exposed areas is increasing with the increasing electron exposure dose used.

Knowledge of the changes of optical properties and etching rates induced by electron beam of different exposure doses can be used for fabricating of optical elements by high resolution electron beam lithography.

Highlights

- Study of change of properties of glassy As35S65 by electron beam exposure.

- Discussion of induced changes of parameters of Tauc-Lorentz oscillator.

- Etching test of glassy As35S65 thin film with recorded image.

- Application of gradient optical model.

- Introduction

Chalcogenide glasses are semiconducting optical materials with promising potential especially in infrared optics [1-3]. It is well known that chalcogenide glasses are sensitive when exposed to electromagnetic radiation or an electron beam [4]. Exposure of the chalcogenide glasses by the electron beam could lead e.g. to the local surface changes in the thickness [5-7], or change of refractive index [7- 11]. Both decrease of refractive index of about 20% under irradiation with 300 keV electron beam [8] and increase of the refractive index of chalcogenide glasses as a consequence of electron beam irradiation [9] was reported. Refractive index change at the surface was found to be n/n = +3.5% [9]. Electron beam irradiated thermally evaporated GeTe thin films first increase and then decrease refractive index when electron exposure dose increase [10]. Moreover decrease in optical band gap and the change in the extinction coefficient have been reported by the same authors [10].

Structural modification which is very likely connected with induced change of optical properties is exploited in the photo-etching [12]. The sensitivity of chalcogenide glass thin films to electron beam exposure can be exploited for practical applications of these materials as an inorganic resist for electron beam lithography [13-16]. The micro/nano-structuring of chalcogenide glasses using different techniques has been reported in previous years [17].

Based on and extended of previous results [18] we present detailed study of the change of the optical properties (refractive index n and extinction coefficient k) and morphological properties (e.g. thickness and surface roughness) of As35S65 chalcogenide glass thin film in dependence on electron exposure dose. This study is focused on usage of spectroscopic imaging ellipsometry as a tool for determination of optical and morphological properties of micro-structured As35S65 chalcogenide glass thin film. The dependence of changes of optical properties on different electron exposure doses can be exploited for fabricating of optical micro/nano elements with on-demand properties.

- Experimental details

The As35S65 chalcogenide glass thin film (d  300 nm) was evaporated onto microscope glass slide and then 11 nm of carbon was deposited onto As35S65 glassy film to make the film conducting. The sample was patterned by e-beam using scanning electron microscope (SEM) model LYRA 3 (Tescan, Czech Republic) at 5 kV accelerating voltage equipped with a micro/nano-pattern generator software. Using an electrostatic beam-blanker, the patterns were written digitally, in a dot-by-dot manner, scanning the writing field. For a systematic analysis of electron beam induced changes the 50 m  50 m squares were recorded by the electron exposure dose changing from 30 C/cm2 to 750 C/cm2 with the step 30 C/cm2.  The sample was stored in dark, dry environment to avoid photo-induced structural changes.

The microscopic maps of the ellipsometric parameters  and  defined identically as in [19-21] were measured by the spectroscopic imaging ellipsometer EP4 from Accurion. The EP4 uses an auto-nulling PCSA (P: polarizer; C: compensator; S: sample, A: analyzer) setup with linear polarizers (P and A) and a quarter-wave-plate as compensator (C) [19-21]. By rotation of P and A to find the minimum signal for each pixel, it is possible to calculate ellipsometric parameters  and  for each pixel. With the optical system on the detector side, the EP4 is able to achieve lateral resolution down to 1 m and to measure different regions on the sample in the field of view simultaneously. Monochromatic light in the range of 390–800 nm with a bandwidth of 5 nm is provided by used monochromator.

Variable angle spectroscopic ellipsometers (VASE J. A. Woollam Co.) was used as a complementary method for the optical characterization of glass substrate and glass substrate with the carbon layer. The ellipsometer was equipped with an automatic rotating analyzer over the spectral range 390 nm – 800 nm, measuring 30 revolutions with wavelength steps of 10 nm at three selected angles of incidence (AOI) (45°, 50° and 55°). WVASE32 software was used for evaluation the measured data.

Electron beam penetration profile simulations were performed using CASINO software [22]. A 300 nm As35S65 thin film with a 11 nm Carbon layer on a SiO2 substrate was modeled at 5 kV acceleration voltage using the default algorithms. The As35S65 chalcogenide glass thin film with latent recorded square patterns was etched in the amine based solution in aprotic solvent. The SEM image of obtained surface structures was recorded using SEM model LYRA 3 (Tescan, Czech Republic) at 5 kV accelerating voltage. The remaining height of the prepared squares was measured using atomic force microscopy technique (Solver NEXT, NT-MDT).

3. Results and discussion

The scattering trajectories of the incident electrons obtained from Monte Carlo simulations with 400 electrons at 5kV using the CASINO v2.48 software [22] are presented in Fig. 1 and model of relative energy of electrons (simulation with 50 000 electrons) using the same software is in Fig. 2 both modeled for the 300 nm of As35S65 film with 11 nm of Carbon layer. From this simulation gradient change of the properties of thin films induced by electron beam can be expected. Although results obtained by homogenous model are in good accordance with the experimental imaging ellipsometry data the gradient model assuming linear change of the refractive index with the thickness is used with respect to the results of Monte Carlo simulation presented at Figs. 1 and 2.

Fig. 1: The scattering trajectories of the incident electrons obtained from Monte Carlo simulations with 400 electrons at 5kV using CASINO v2.48 software [22]. The size of the area depicted is 311 nm (depth) x 462 nm (width).

Fig. 2: Model of relative energy of electrons (simulation with 50 000 electrons) using CASINO v2.48 software [22]. The size of the area depicted is 256 nm (depth) x 360 nm (width).

The pixelshot tool of the Accurion software was applied to obtain  map of the glassy As35S65 thin film (d  300 nm) with 11 nm of Carbon evaporated onto microscope glass slide with the square pattern recorded by electron beam with different exposure doses for wavelength 380 nm. The result is depicted at Fig. 3 together with the electron beam exposure used as a number. Clearly there is visible change in the measured  parameter for different squares.

Fig.3:  map of the glassy As35S65 thin film (d  300 nm) with 11 nm of Carbon evaporated onto microscope glass slide with the square pattern recorded by electron beam with different exposure doses for wavelength 380 nm. Numbers express electron beam exposure used.

A sample model used to analyze the raw ellipsometry data consists of i) a semi-infinite glass substrate, ii) a layer with the linear change of the refractive index with the thickness representing the measured square of glassy As35S65 film, iii) a Carbon layer iv) surface roughness modeled by a Bruggeman type effective medium approximation [23] with 50% of voids and 50% of Carbon layer underneath and v) air as the ambient medium (see Fig. 4).

Fig. 4: Gradient optical model used to fit the ellipsometry data

Optical constants of the glass substrate were obtained by measurement of an uncoated glass substrate. Optical constants and the thickness of the Carbon layer were obtained by measurement of a glass substrate coated with the carbon layer at the same conditions as was used for Carbon coating of As35S65 layer afterwards. In the first approximation both optical properties of Carbon layer as well as its thickness (11 nm) are supposed to be unchanged by the electron beam.

The change of the polarization state is usually expressed by two parameters, amplitude ratio  and phase shift , that are defined using the Fresnel reflection coefficients for p- and s- polarized light:

rprs=tanψ∙expiΔ (1)

Spectroscopic ellipsometry is an indirect optical characterization method, where numerical ellipsometric model needs to be assumed to obtain physical values, like complex refractive index and thickness out of measured exp and exp spectra. In the model structure, the model dielectric function for each square of glassy As35S65 which define its optical constants is Tauc-Lorentz oscillator and thickness of this layer as well as thickness of the surface roughness are assumed. Using proposed model structure corresponding values of mod and mod can be calculated.

Short wavelength absorption edge (SWAE) for amorphous materials is commonly modeled by Tauc-Lorentz (TL) oscillator [24-25]

ε2=A∙E0∙C∙E-Egopt2E2-E022+C2∙E2∙1E for E>Egopt (2)

ε2=0 for E≤Egopt (2)

ε1=2πPEg∞ξ∙ε2ξξ2-E2dξ (2)

The layer is transparent below optical bandgap Egopt in TL model. So called Tauc plot obtained from transmission measurement can be alternatively used for the estimation of Egopt.  Other used parameters A, E0, C stand for amplitude, peak position and broadening of the oscillator respectively.

Moreover the linear change of the refractive index with the variable variation (in percent) between the refractive index at the top of the layer and the bottom of the layer is assumed.

In our case, the measured spectroscopic ellipsometry parameters, exp and exp fitted against the designed model in the spectral range from 390 nm to 800 nm using the mean square error (MSE) given in the following expression:

MSE=12N-Mi=1Nψimod-ψiexpσψ,iexp2+Δimod-ΔiexpσΔ,iexp2 (3)

where N is the number of measured pairs of ellipsometric parameters exp and exp and M represents the total number of fitted parameters. σψ,iexp and σΔ,iexp are then the estimated experimental error of exp and exp, respectively. Ellipsometric data measured for all three angles of incidence 45°, 50° and 55° were used in the fit simultaneously.

Fig. 5 shows the comparison of ellipsometry parameters,  (upper part) and  (lower part) for an AOI of 50° in the spectral range from 390 to 800 nm for native As35S65 (untreated with the electron beam, black squares) and for the square of glassy As35S65 irradiated with electron exposure dose 750 µC.cm-2 (blue circles).

Fig. 5: Measured values of ψ (upper part) and Δ (lower part) for native As35S65 sample (black squares) and for the square irradiated with electron exposure dose 750 µC.cm-2 (blue circles). The best fit for the angle of incidence 50° is shown by solid lines.

Fig. 6 shows determined dispersion of the refractive index, n (upper part), and extinction coefficient, k (lower part), of native As35S65 film at bottom of the film (red) and at the top of the film (black) and the electron exposed square irradiated with electron exposure dose of 750 µC.cm-2 at bottom of the film (purple) and at the top of the film (blue). The refractive index for the native As35S65 film is almost the same within the depth of the film. Refractive index is generally increasing with the increasing electron exposure dose (greater increase is detected at the top of the film) which suggests densification of glass structure. The onset of SWAE is moving toward lower photon energies. The Kramers–Kronig relations [26-27] describe the relationship between real (refractive index n) and imaginary (extinction coefficient k) part of complex refractive index which is again nearly the same for the native As35S65 film and extinction coefficient at the top of the film is slightly larger than extinction coefficient at the bottom of the film for electron exposed square irradiated with electron exposure dose of 750 µC.cm-2.

Fig. 6: Determined refractive index n (upper part), and extinction coefficient k (lower part), as a function of photon energy for native As35S65 sample at bottom of the film (red) and at the top of the film (black) and for the square irradiated with electron exposure dose 750 µC.cm-2 at bottom of the film (purple) and at the top of the film (blue).

Ellipsometry data obtained by imaging ellipsometer EP4 from all 25 squares recorded into As35S65 layer with different electron exposure dose has been fitted with the model described earlier with MSE below 5 for all measured squares. Fig. 7 (upper part, black squares) shows thickness of the studied electron beam irradiated square as a function of electron exposure dose. The thickness of the films tends to slightly decrease with the increasing electron exposure dose supporting the idea of the densification of the glass structure induced by electron beam exposure mentioned earlier. It is worth mentioning that this 2 nm ( 1 %) decrease of layer thickness is comparable with thickness nonuniformity of the layer. In the Fig. 7 (upper part, blue circles for the bottom of the film and blue triangles for the top of the film) there is also the dependence of the refractive index at 750 nm (where the layer is transparent) on the electron exposure dose used. As expected from results described earlier (see Fig. 6 (upper part)) refractive index is increasing with increasing electron exposure dose and refractive index for the top of the film increase more sharply. The difference between bottom and top of the film is more pronounced for electron exposure dose higher than 110 µC.cm-2. In the Figs. 7-10 electron exposure dose = 0 is used for native As35S65 layer. By the electron exposure refractive index for 750 nm increases from 2.39 (native layer) to 2.46 (electron exposure dose = 750 µC.cm-2, top of the film). This  3% increment in the refractive index of As35S65 chalcogenide glass was reported for As2S3 before [9].

Refractive index at 450 nm (where the layer absorbs) is increasing with electron exposure dose similarly to the same dependence at 750 nm (see Fig. 7 (lower part, black squares and black circles)). Extinction coefficient at 450 nm increases with the electron exposure dose suggesting that the changes in the material induced by electron beam increase absorption of the material (see Fig. 7 (lower part, blue circles and blue diamonds)). Again described increase is more pronounced for the top of the film. By the electron beam exposure refractive index at 450 nm increases from 2.78 (native layer) to 2.90 (electron exposure dose = 750 µC.cm-2, top of the film).

Fig. 7: Dependence of the thickness of the glassy As35S65 sample irradiated by electron beam on electron exposure dose (upper part, black squares) together with  dependence of the refractive index at 750 nm of the glassy As35S65 sample irradiated by electron beam on electron exposure dose for the bottom of the film (upper part, blue circles) and for the top of the film (upper part, blue triangles). Dependence of the refractive index at 450 nm of the glassy As35S65 sample irradiated by electron beam on electron exposure dose for the bottom of the film (lower part, black squares) and for the top of the film (lower part, black circles) together with dependence of the extinction coefficient at 450 nm of the glassy As35S65 sample irradiated by electron beam on electron exposure dose for the bottom of the film (lower part, blue triangles) and for the top of the film (lower part, blue diamonds). Lines are used as an eye guide.

Tauc-Lorentz oscillator used for modeling complex dielectric function of the optical properties of glassy As35S65 irradiated with electron beam with different exposure dose has several parameters (see eq. 2). The range of the transparency is determined by the parameter Egopt which is generally decreasing with increasing electron exposure dose (“electron exposure induced bleaching”) (see Fig. 8, black squares). The dependence of variation of the refractive index within the sample thickness is increasing from the zero (homogenous sample) to 2 % for the exposure dose higher than 290 µC.cm-2 (see Fig. 8, blue circles). From the obtained data variation of the refractive index become nonzero for exposure dose higher than 150 µC.cm-2 (see Fig. 8, blue circles).

Fig. 8: Dependence of the parameter Egopt (optical bandgap) of the TL oscillator of the glassy As35S65 thin film irradiated by electron beam (black squares) and dependence of the variation in refractive index within the sample thickness (blue circles) on electron exposure dose Lines are used as an eye guide.

Parameters A, E0, C of TL oscillator remains nearly constant for all electron exposure dose used. Mean value of these parameters together with the error of their fit is at Table 1.

| Parameter | A (eV) | E0 (eV) | C (eV) |
| --- | --- | --- | --- |
| Mean value error | 186 30 | 3.9 0.3 | 4.8 0.9 |

Table 1: Mean value of parameters of TL oscillator together with their error for all studied electron exposed areas

Considering the error in determining of surface roughness about 0.1 nm we can conclude that surface roughness 1.5 nm is not significantly changing with electron exposure dose.

Parameter B1/2 which is the slope of the dependence of (E)1/2 as a function of photon energy E is connected to the width of the localized states near the mobility edges E. E depends on the degrees of disorder and defects present in the amorphous structure (Mott and Davis [28-29] and Tauc [30] models), in particular, differences in coordination number in amorphous state with respect to crystalline state [31-32], and can be taken as a measure of a disorder. Calculation of the parameter B was done in the similar matter as in our previous work (please see pages 444-445 in ref. [33]).

Influence of the used electron exposure dose decrease the sample disorder (the increase of parameter B1/2). The width of localized states can be compared with native layer for all measured samples as (ΔEdx/ΔEnative) = (Bnative/Bdx)/(ndx/nnative) where subscript dx stands for exposure dose = x C.cm-2. The dependence of the slope of SWAE (B1/2) on the exposure dose is depicted at upper part of Fig. 9 for the bottom of the film (squares) and for the top of the film (circles). The dependence of the E ratio on the exposure dose for the bottom of the film (squares) and for the top of the film (circles) is depicted at lower part of Fig. 9. The E ratio was calculated using the refractive index for 2.43 eV. From these results shrinking of the width of localized states (more pronounced at the top of the film) due to electron exposure dose can be observed. Maximum decrease of disorder in the material approximately of about 14% in comparison with native sample is observed.

Fig. 9: Dependence of the slope of SWAE for the bottom of the film (squares) and for the top of the film (circles) (upper part) together with the dependence of the ratio of the width of localized states for the bottom of the film (squares) and for the top of the film (circles) (lower part) of the glassy As35S65 sample irradiated by electron beam on electron exposure dose. Lines are used as an eye guide.

The parameters of the Wemple-DiDomenico model [34-35] E0 and Ed can be calculated from the linear regression of dependence n2-1-1 against E2 in the semi-transparent part of spectra below the bandgap (1.5 < E < 2.3 eV) in the similar matter as in our previous work (please see pages 443-444 in ref. [33]).

Fig. 10 shows the variation of Ed (black squares for the bottom of the film and black circles for the top of the film) and E0 (blue triangles for the bottom of the film and blue diamonds for the top of the film) as a function of electron exposure dose used for structuring of the As35S65 films. Ed is slightly increasing at the top of the film and slightly decreasing for the bottom of the film with the electron dose used. Although the differences are small this results suggest that exposure dose change the chemical surrounding around the cation differently at the top of the layer and at the bottom of the layer. E0 is ~ 4.7 eV for native film and is decreasing with electron exposure dose equally for the bottom (blue triangles) and for the top (blue diamonds) of the film. Parameter E0 (distance of centroids of valence and conduction band) is associated with optical bandgap (E0≈1.5+1.25Egopt) [36-37]. From the decrease of the parameter E0 with increasing electron exposure dose, the decrease in the optical bandgap (red shift) could be deduced. The same trend can be also seen from the parameters of the Tauc-Lorentz oscillator (see Fig. 8, black squares).

Fig. 10: Dependence of the Wemple-DiDomenico parameter Ed for the bottom of the film (black squares) and for the top of the film (black circles) and E0 for the bottom of the film (blue triangles) and for the top of the film (blue diamonds) of the glassy As35S65 sample irradiated by electron beam on electron exposure dose. Lines are used as an eye guide.

The As35S65 thin film with recorded image was etched in amine based solution in aprotic solvent for the time needed to dissolve the native (unexposed) thin film (Fig. 11). Due to the local structural changes induced by the electron beam the dissolution rate of the exposed areas is much slower in comparison with unexposed areas. The thickness of the remaining thin film increases with increasing electron exposure dose used up to exposure dose  210 µC.cm-2. Higher exposure doses do not increase the thickness of remaining thin film.

According to [18], the structural changes induced by electron beam in thermally evaporated As35S65 thin films are most likely similar to those induced by super bad-gap light irradiation where exposure results in structural polymerization (breaking of homopolar bonds As-As and S-S while forming more chemically resistant AsS3/2 polymer structure). Additionally XPS studies of electron beam exposed As35S65 thin films [38] prove decrease of sulfur content on the surface of thin film with increasing exposure dose, which makes electron beam exposed areas further more chemically resistant.

Fig. 11: SEM image of thin film with recorded image etched in amine based solution in aprotic solvent (upper part). Dependence of the remaining thickness of the thin film after the etching on the electron exposure dose used (lower part).

- Conclusion

Spectroscopic ellipsometry study on 50 µm  50 µm squares recorded by electron beam with various exposure doses (30 – 750 µC.cm-2) to glassy As35S65 thin films were conducted by imaging ellipsometry. The refractive index and extinction coefficient of exposed areas over spectral range from 390 nm to 800 nm were obtained by the best fit of imaging ellipsometry data. Dielectric functions of those electron beam exposed square areas were modelled by Tauc-Lorentz oscillator describing short wavelength absorption edge. Gradient optical model with the refractive index changing linearly within the layer thickness was used. Evaluation of parameters of Tauc-Lorentz oscillator revealed decrease of energy bandgap with the increasing electron exposure dose. Refraction index increases maximally of about 0.1 ( 4 %) and energy bandgap decreases maximally of about 0.02 eV ( 1 %) as a consequence of electron beam exposure. More pronounced changes were detected at the top of the film.

The decrease of local disorder with electron exposure dose maximally by about 14 % was quantified Using a Mott-Davis model in the vicinity of the absorption edge (2.4 < E < 3.0 eV). The Wemple-DiDomenico model in the semi-transparent spectrum (1.6 < E < 2.3 eV) reveal possible different chemical surrounding of the cation at the top of the film and at the bottom of the film induced by electron beam exposure.

In this article, the possibilities of imaging spectroscopic ellipsometry especially for amorphous As35S65 with total 25 squares (50 x 50 µm) recorded by electron beam with various electron exposure doses had been discussed. Thin film with recorded image was also etched in amine based solution in aprotic solvent. With this knowledge the micro-structured objects with known optical properties can be prepared.

Acknowledgments

Authors appreciate financial support from project No. 16-13876S financed by the Grant Agency of the Czech Republic (GA CR) as well as support from the grants LM2015082 and ED4.100/11.0251 from the Ministry of Education, Youth and Sports of the Czech Republic. The work was supported from European Regional Development Fund-Project „Modernization and upgrade of the CEMNAT“ (No. CZ.02.1.01/0.0/0.0/16_013/0001829).

References

[1] A. Stronski, M. Vlcek, A. Sklenar, Photoinduced structural changes in As₁₀₀₋xSx layers, Semiconductor Physics, Quantum Electronics & Optoelectronics 3 (2000) 394-399.

[2] A. Zoubir, M. Richardson, C. Rivero, A. Schulte, C. Lopez, K. Richardson, N. Hô, R. Vallée, Direct femtosecond laser writing of waveguides in As2S3 thin films, Opt. Lett. 29 (2004) 748-750.

[3] S. Song, S.S. Howard, Z. Liu, A. O. Dirisu, C. F. Gmachl, C. B. Arnold,  Mode tuning of quantum cascade lasers through optical processing of chalcogenide glass claddings  Appl. Phys. Lett., 89 (2006) 041115.

[4] K. Tanaka, K. Shimakawa, Amorphous Chalcogenide Semiconductors and Related Materials. Springer 2011.

[5] J.S. Romero, A.G. Fitzgerald, K. Mietzsch, Electron irradiation induced expansion in amorphous chalcogenide films, J. Appl. Phys. 91 (2002) 9572-9574.

[6] K. Tanaka, Electron beam induced reliefs in chalcogenide glasses, Appl. Phys. Lett. 70 (1997) 261-263.

[7] O. Nordman, N. Nordman, N. Peyghambarian, Electron beam induced changes in the refractive index and film thickness of amorphous AsxS100−x and AsxSe100−x films, J. Appl. Phys. 84 (1998) 6055-6058.

[8] D.P. San-Roman-Alerigi, D.H. Anjum, Y. Zhang, X. Yang, A. Benslimane, T. K. Ng, M.N. Hedhili, M. Alsunaidi, B.S. Ooi, Electron irradiation induced reduction of the permittivity in chalcogenide glass (As2S3) thin film, J. Appl. Phys. 113 (2013) 044116.

[9] T. Suhara, H. Nishihara, and J. Koyama, Electron-beam-induced refractive-index change of amorphous semiconductors, Jpn. J. Appl. Phys. 14 (1975) 1079–1080.

[10] D. Sarkar, G. Sanjeev, M.G. Mahesha, Influence of electron beam irradiation on structural and optical properties of thermally evaporated GeTe thin films, Radiation Physics and Chemistry 98 (2014) 64–68.

[11] S. A. Sergeev, M. S. Iovu, O. V. Iaseniuc, Electron-beam recording of patterns in chalcogenide films, Proc. SPIE 9258, Advanced Topics in Optoelectronics, Microelectronics, and Nanotechnologies VII, 92580S (20 February 2015).

[12] S.A. Zenkin, S.B. Mamedov, M.D. Mikhailov, E.Yu. Turkina, I.Yu. Yusupov, Mechanism for interaction of amine solutions with monolithic glasses and amorphous films in the As-S system, Glass Phys. Chem. 23 (1997) 393-399.

[13] K.L. Chopra, L.K. Malhotra, K.S. Harshvardhan, B. Singh, Radiation-induced microlithographic effects in amorphous chalcogenide films, Proceedings - Electrochemical Society (Proc. Symp. Inorg. Resist Syst.) 82-9 (1982) 129-45.

[14] B. Singh, S.P. Beaumont, P.G. Bower, C.D.W. Wilkinson, New inorganic electron resist system for high resolution lithography, Appl. Phys. Lett. 41 (1982) 889-891.

[15] B. Singh, S.P. Beaumont, P.G. Bower, C.D.W. Wilkinson, Sub‐50‐nm lithography in amorphous Se‐Ge inorganic resist by electron beam exposure, Appl. Phys. Lett. 41 (1982) 1002-1003.

[16] J. Teteris, Amorphous As–S–Se semiconductor resists for holography and lithography, J. Non-Cryst. Solids 299–302 (2002) 978-982.

[17] H. Jain, M. Vlcek, Glasses for lithography, J. Non. Cryst. Solids 354 (2008) 1401–1406.

[18] J.R. Neilson, A. Kovalskiy, M. Vlcek, H. Jain, F. Miller, Fabrication of nano-gratings in arsenic sulphide films, J. Non. Cryst. Solids 353 (2007) 1427-1430.

[19] R.M. Azzam, N.M. Bashara, Ellipsometry and Polarized Light,Sole distributors for the USA and Canada, Elsevier Science Publishing Co., Inc., North-Holland, 1987.

[20] H. Fujiwara, Spectroscopic Ellipsometry: Principles and Applications, John Wiley & Sons, Chichester, England; Hoboken, NJ, 2007.

[21] H. Tompkins, E.A. Irene, Handbook of Ellipsometry, William Andrew, 2005.

[22] D. Drouin, A.R. Couture, D. Joly, X. Tastet, V. Aimez, R. Gauvin, CASINO V2.42: a fast and easy-to-use modeling tool for scanning electron microscopy and microanalysis users, Scanning 29 (2007) 92-101.

[23] D. A. G. Bruggeman, Berechnung verschiedener physikalischer Konstanten von heterogenen Substanzen. I. Dielektrizitätskonstanten und Leitfähigkeiten der Mischkörper aus isotropen Substanzen, Ann. Phys. (Leipzig) 24 (1935) 636-664.

[24] G. E. Jellison, Jr., F. A. Modine, Parameterization of the optical functions of amorphous materials in the interband region, Appl. Phys. Lett. 69 (1996) 371-373.

[25] G. E. Jellison, Jr., F. A. Modine, Erratum: Parameterization of the optical functions of amorphous materials in the interband region, Appl. Phys. Lett. 69 (1996) 2137-2137.

[26] R. de L. Kronig. J. Opt. Soc. Am. 12 (1926) 547.

[27] H.A. Kramers, La diffusion de la lumière par les atomes. Atti del Congresso Internationale dei Fisici, (Transactions of Volta Centenary Congress), Como, 2 (1927) 545-557.

[28] N.F. Mott, E.A. Davis. Electronic Processes in Non-Crystalline Materials. Clarendon Press, Oxford (1979);

[29] E.A. Davis, N.F. Mott, Conduction in noncrystalline systems.  V.  Conductivity, optical absorption, and photoconductivity in amorphous semiconductors, Philosophical Magazine 22 (1970) 0903-0922.

[30] J. Tauc. In Amorphous and liquid semiconductors (J. Tauc ed.). Plenum Press, New York (1974).

[31] S.R. Ovshinsky, D. Adler, Local structure, bonding, and electronic properties of covalent amorphous semiconductors, Contemporary Physics 19 (2006) 109-126.

[32] M.L. Theye, Optical properties of amorphous germanium, amorphous silicon, and amorphous III-V compounds, Proceeding of the Fifth International Conference on Amorphous and Liquid Semiconductors, Garmisch- Partenkirchen 1 (1974) 479-498.

[33] P. Janicek, S. Slang, K. Palka, M. Vlcek, Spectroscopic ellipsometry characterization of spin-coated Ge25S75 chalcogenide thin films, Pure and Applied Chemistry 89 (2017) 437-449.

[34] S.H. Wemple, Refractive-Index Behavior of Amorphous Semiconductors and Glasses, Phys. Rev. B 7 (1973) 3767-3777.

[35] S.H. Wemple, M. DiDomenico, Behavior of the Electronic Dielectric Constant in Covalent and Ionic Materials, Phys. Rev. B 3 (1971) 1338-1351.

[36] K. Tanaka, Optical properties and photoinduced changes in amorphous As-S films, Thin Solid Films 66 (1980) 271-279.

[37]  H. Ticha, L. Tichy, Semiempirical relation between non-linear susceptibility (refractive index), linear refractive index and optical gap and its application to amorphous chalcogenides,  J. Optoelectron. Adv. Mater. 4 (2002) 381-386.

[38] A. Kovalskiy, J.R. Neilson, A.C. Miller, F.C. Miller, M. Vlcek, H. Jain: Comparative study of electron- and photo-induced structural transformations on the surface of As35S65 amorphous thin films, Thin Solid Films 516 (2008) 7511–7518.